Annexe

| Annexe 1: Intelligent Module Design [20] The Siemens SM110/SM100 single crystalline solar module is available in a framed and a laminate version. Both modules feature a rugged laminate design and PowerMax® solar cells to provide maximum energy production throughout the day. The module has a rated output of 110 WP/100 WP and is available in a 12 volt and as the SM1 10-24/SM100-24 in a 24 volt version. The efficient design of the SM1 10/SM100 module, with its large surface area, is ideally suited for medium and high output applications. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SM110/SM100 |  | SM110 |  |  | SM100 |  |
| Electrical Parameters1 |  | 12V |  | 24V | 12V | 24V |
| Maximum power rating, Pmax | [Watts] | 110 |  | 110 | 100 | 100 |
| Minimum power rating, Pmin | [Watts] | 100 |  | 100 | 90 | 90 |
| Rated current, Imp | [Amps] | 6.3 |  | 3.15 | 5.9 | 2.95 |
| Rated voltage, Vmp | [Volts] | 17.5 |  | 35.0 | 17.0 | 34.0 |
| Short circuit current, Isc | [Amps] | 6.9 |  | 3.45 | 6.5 | 3.25 |
| Open circuit voltage, Voc | [Volts] | 21.7 |  | 43.5 | 21.0 | 42.0 |
| Thermal Parameters |  |  |  |  |  |  |
| Nominal operating cell temperature2 | [°C] | 45(+or-)2 |  |  |  |  |
| Change of Isc with temperature |  | +1.2mA/°C (+0.04%/K) |  |  |  |  |
| Change of Voc with temperature |  | -0.0775 Volts/°C (-0.34%/K) |  |  |  |  |
| Qualification Test Parameters3 |  |  |  |  |  |  |
| Temperature cycling range | [°C] | -40 to +85 |  |  |  |  |
| Humidity, freeze, damp heat condition | [% RH] | 85 |  |  |  |  |
| Maximum system voltage | [Volts] | 1000 per ISPRA (EC) 600 per UL1703 |  |  |  |  |
| Wind loading or surface pressure | [N/m2] (lb/sqft) | [2400] (50) |  |  |  |  |
| Maximum distortion4 | [degrees] | 1.2 |  |  |  |  |
| Hailstone impact withstand (diameter @ velocity) | [mm @ m/s] (in @ MPH) | 25 @ 23 (1.0 @ 52) |  |  |  |  |
| Physical Parameters |  |  |  |  |  |  |
| Number of cells in series |  | 72 |  |  |  |  |
| Length | [mm] (in) | 1316 (51.8) |  |  |  |  |
| Width | [mm] (in) | 660 (25.98) |  |  |  |  |
| Depth (without box) | [mm] (in) | 40 (1.6) |  |  |  |  |
| Weight | [kg] (lb) | 11.5 (25.1) |  |  |  |  |